## Slide 1: Aspects of heat transfer from ferrite to metal in ultra-high vacuum
F. Caspers & M.J. Barnes

## Slide 2: Near-Field Effects
“Contact”
Classical radiation regime
C.M. Hargreaves, “Electromagnetic proximity effects and their consequences for radiation shielding”, Fifth Cryogenic Engineering Conference.
Plot shows:
Red area: classical radiation regime, for spacing between black surfaces greater than one wavelength.
Blue area: energy transfer with both evanescent waves AND classical travelling waves. One can describe this phenomenon as infra-red tunnelling – which works well even between shiny surfaces where classical heat transfer by radiation would be very low (due to low emissivity).
There is a smooth transition between radiation and contact regimes – by applying mechanical pressure, size of the gap is simply reduced.

## Slide 3: 2D FEM Modelling of MKI Kicker Magnet (1)
ε_tank=0.05
ε_ferrite=0.9
Tank Emissivity
Maximum ferrite temperature [˚C]
Maximum ferrite temperature is greatly dependent upon emissivity of inside of metal tank (ferrite emissivity: 0.8 - 0.9): high emissivity gives good thermal radiation.
Thermal modelling courtesy of Marco Garlasche.
MKI Strategy Meeting, 11/05/2012.
100W power deposition in MKI ferrite yoke

## Slide 4
Convection coefficient [W/m2-K @ 22 °C]:
5 0.25 0
Analyses performed for different external tank convection coefficients (100W power deposition in MKI ferrite yoke)
2D FEM Modelling of MKI Kicker Magnet (2)
Tank Emissivity
Maximum ferrite temperature [˚C]
5
0.25
0
Maximum ferrite temperature is also greatly dependent upon external cooling of tank – this is especially true for high power depositions.
ε_tank=0.05
ε_ferrite=0.9
Thermal modelling courtesy of Marco Garlasche.
MKI Strategy Meeting, 11/05/2012.

## Slide 5: Measurements of MKI12 tank emissivity following an ion bombardment treatment
Chart: Distance inside the tank [cm]
| 40 | 100 | 100 | 100 | 200 | 260
bottom | 0.55556 | 0.74144 | 0.26562 | 0.16529 | 0.24194 | 0.58273
left | 0.31408 | 0.36996 | 0.46269 | 0.46021 | 0.66176 | 0.49296
right | 0.72624 | 0.76307 | 0.58621 | 0.69403 | 0.68657 | 0.55944
top | 0.15571 | 0.13821 | 0.16996 | 0.15 | 0.20472 | 0.15571
Data courtesy of Wim Weterings.
MKI Strategy Meeting, 31/10/2012
Tanks emissivity before treatment ~0.1: in places emissivity is increased to 0.7. Second treatment to be applied to try and achieve uniformly high emissivity on inside of tank.

## Slide 6: How to Improve Heat Transfer
Increase emissivity of surface of “heat source” and “heat sink”;
We cannot easily braze to a metallic surface – because of differential expansion coefficients: only feasible with small volumes and mechanical pre-stress (delicate and risky).
Alternative solutions for heat transfer include:
  ion bombardment of metallic surface to increase emissivity (see next slide);
    Vacuum evaluation required.
    Bake-out evaluation required.
  plasma spray technology of thin ferrite layers (avoids expansion problems, but cannot be cut mechanically). Emissivity measured to be ~0.85;
    Vacuum evaluation required.
Where applicable: direct liquid cooling of heat source (not necessarily applicable where there is high voltage).