## Slide 1
MKI8BCD: Temp_Tube_Up. May 1, 2012 to 21 Nov. 2012
Maximum value of Temp_Tube_Up of MKI8B, since May 1st, has been fairly consistent;
Maximum value of Temp_Tube_Up of MKI8D, since May 1st, has been fairly consistent, but is slightly lower for the new MKI8D (changed TS#3);
Maximum value of Temp_Tube_Up of MKI8C, until TS#3, was generally < 120˚C, with one excursion to ~150˚C on 27/08. Since TS#3 the temperature has approached 180˚C at times (but not always).
TS#3
MKI8C_TEMP_TUBE_UP
MKI8D_TEMP_TUBE_UP
MKI8B_TEMP_TUBE_UP

## Slide 2
MKI8C: Temp_Tube/Magnet_Up. May 1, 2012 to 21 Nov. 2012
Before TS#3 maximum value of Temp_Tube_Up of MKI8C was generally < 120˚C, and Temp_Magnet_Up approached 50˚C.
Since TS#3 increased heating of maximum value of MKI8C Temp_Tube_Up has increased temperature of MKI8C Temp_Magnet_Up (by thermal radiation).
TS#3
MKI8C_TEMP_TUBE_UP
MKI8C_TEMP_MAGNET_UP

## Slide 3
Results:
TRings [°C] experimental | T [°C] meas. experimental | PRings FEM | TRings [°C] FEM | T [°C] plate FEM | T [°C] yoke FEM
130 | 55 | 8 | 127 | 64 | 109.2
160 | 60 | 12 | 155 | 71 | 111.9
Given PRings such that TRings is met, does the model predict well the first plate temperature?
Initial condition for analyses: PCshape_EQ=350W , PRings=0
Tplate overestimated, but increase due to ferrite rings is possible
First plate reaches 52°C
Case PRings=8W
Slide courtesy of Marco Garlasche
ΔT=7˚C
ΔT=5˚C
Corresponding predicted ΔT of ferrite: ~3˚C

## Slide 4
MKI8C: Magnet Delay and Rise-Time Since TS#3
TS#3
When the magnet yoke temperature is below the Curie temperature the slope of the above curves are defined by the temperature dependence of the MKI capacitors.
Abrupt changes of above slopes are most likely due to radiated power from MKI8C_Tube_Up, due to an increase of the measured temperature of MKI8C_Magnet_Up, increasing the temperature of ~10% (guestimate) of the ferrite yoke.