## Slide 1
Thermal evaluation on VMTSA heating
M. Garlasché, A. Bertarelli
Acknowledgements: G. Bregliozzi, E. Metral

## Slide 2
Short recap
VMTSA configuration
FEM Model
Results
Summary

## Slide 3
…Opening of the concerned vacuum sectors during Xmas break 2011-2012, have shown that the stainless steel spring is deformed and brazed to the Cu/Be RF fingers and that the RF fingers are permanently deformed. The estimated temperature reached during operation is ~ [800÷]1000 °C…
Short recap
[1]
[2]
[1] LMC 16-11-11, V. Baglin
[2] EDMS LHC-VMTSA-EC-0001, V. Baglin

## Slide 4
PRF,fingers(40mm gap)~650W
PRF,fingers(50mm gap)~460W
Is RF power deposition compatible with expected failure Temperatures?
Limit for power value?
[3]
Short recap
[3] LRFF Meeting 30-10-2012, O. Kononenko
Old configuration (long RF fingers)

## Slide 5
2x ion pump with jackets
Eventual cover
4x screws for support
VMTSA Configuration
Material:
Stainless Steels (316L/LN,304L)
CuBe
C10100 (OFE Cu)
..Interesting features for thermal analysis of long fingers configuration..
Rh dep.
Ag dep.

## Slide 6
2 Fold Symmetry
No central pipe support (LHCVMTSA0008)
No heat evacuation to pumps & ground/top
Components in | Th. Cond [W/m-K] | Emiss. | Emiss. (Lit.)
C17410 | 233 | 0.05 | 
Ag coating | - |  | 0.03
Rh coating | - |  | 0.03-0.1
C10100 | 400 |  | 0.05-0.1
SS. 304L | 15 | 0.3 | 0.3-0.4
SS. 316/LN |  |  | 
Ideal thermal contact
Free (5 W/m2K @ 22C) external convection on all surfaces
Ideal th. Contact between fingers and spring mockup
Balanced heat exchange scenario with maximum spring temperature
Evenly distributed Power deposition
FEM Model
Function of T

## Slide 7
Nonlinear static thermal analysis performed for different RF power cases
PRF [W] | T finger max [°C] | T spring [°C]*
40 | 190 | 188
160 | 498 | 471
400 | 806 | 706
480 | 878 | 752
(*) indication, as real geometry is not respected
For higher PRF, convergence is critical w.r.t time effective simulation...
Results
Case shown: 480W

## Slide 8
Fingers heat evacuation can be approximated as following:
Geometry
Materials conductivity
Contacts
Geometry (view factors, surfaces)
Materials emissivity
Comp. position
T [°C]
PRF [W]
Max interpolation error~ 6°C
Results

## Slide 9
T [°C]
Results
PRF [W]
Carefully extrapolating for higher P values..
Temperatures expected for 650W (40mm gap)? 990°C
Power expected for 1000°C? 670W

## Slide 10
Results
T [°C]
PRF [W]
What could be a reasonable Power limit due to fingers failure? 100°C PRF=18W
[4]
C17410
[4] LRFF Meeting 03-04-2012, S. Calatroni
Stress relaxation resistance (75% stress)

## Slide 11
Conclusions
Simplified model! Watch out especially regarding spring temperature
Failure temperatures estimate are compatible with PRF expected
1000°C reached with PRF=670W
PRF=18W limit for 100°C on fingers

## Slide 12: Back Up

## Slide 13
Temp. plots for 480W case

## Slide 14
Temp. plots for 40W case