## Slide 1: Review of ferrites used at CERN to damp HOMs: TE/ABT equipment
M.J. Barnes and W. Weterings
05 June 2012

## Slide 2
TE/ABT HOM Damping Ferrites
Kicked Beam
TMR connection
entrance box connection
capacitor
ferrite
yoke
ground
plate
ground
plate
HV plate
HV plate
Beam impedance reduction ferrite
(lossy + low-loss)
Beam impedance reduction ferrites
(lossy + low-loss)
Damping resistor (now at both ends)
Screen conductors soldered to “ground”
Screen conductors capacitively coupled to “ground”
Beam impedance reduction ferrites
(lossy + low-loss)
Beam impedance reduction ferrites
(lossy + low-loss)
Only HOM damping ferrites in TE/ABT equipment, that we are presently aware of, are in the MKI tank.
Notes: NiZn: 4B3; medium permeability.
NiZn: 4M2;
MnZn: 3E25

## Slide 3: MKI: HOM Damping Ferrites
Each of the two sets of MKI HOM damping ferrites (a.k.a. “beam impedance reduction ferrites”) consists of 9 toroidal cores: 4 or 5 of each of Ferroxcube T87/54/14-4M2 and T87/54/14-4B3 per set.
Treatment - after surface treatment by Marina:
  Treatment in air in an oven, ramped at 50°C /hour to 1000°C, plateau of 2 hours, then reduction in temperature at 50°C/hour.
  Redo the same treatment but under vacuum.

## Slide 4: Other HOM Damping Materials…
The SPS septa and protection elements do not use ferrites to damp HOM’s, but do use a ceramic capacitor with carbon deposit resistors.