## Slide 1: Ferrites in BE-BI
Preliminary Data
Compiled by R.Veness with information from W.Andreazza, B.Dehning, D.Gerard, R.Jones, L.Soby

## Slide 2: Introduction
Definition
  In this context, a ‘ferrite’ is any material used for suppressing HOMs (i.e., could also be SiC or other)
Completeness
  It was not possible to collect a complete picture of ferrite use in BI, as:
    The time available was limited
    Documentation for some systems is not complete or available

## Slide 3: Ferrites in Wire Scanners
PS FWS
  5 new tanks installed in 2011/12
    ‘FERROXCUBE’ PLT 100/100/6/H-4SD60 as per EDH 2542526
    UHV cleaned at CERN, then heat-treated at 400 C
    2 blocks installed per tank
SPS BWS
  No recent modifications made to ferrites
    ‘FERROXCUBE’ 4S60 (same as above?)
    Treatment and quantity TBC

## Slide 4: Ferrites in Wire Scanners
PSB and LHC
  Information less clear for the moment
    Either 4S60 or Philips ferrites (from F.Caspers)
    Baked-out, but temperature TBC
    Quantity TBC

## Slide 5: Wall Current Monitors
PS WCMs
  Installed in SS03 and SS95
    Material T240/160/20-8C11
    5 rings in each WCM
    Treatment TBC
    Also contain RF-absorber tiles
CTF3 WCMs
  5 pieces in 10 GHz WCMs

## Slide 6: Other
PS CODD pick-ups
  Each pick-up contains 2 tiles of RF-absorber ferrites