## Slide 1: HiRadMat Tests on Collimator Materials: Preliminary Results and RF Implications BE-ABP-ICE Section Meeting 07.11.2012 A. Bertarelli on behalf of the LCMAT Design Team (A. Bertarelli, E. Berthome, F. Carra, A. Dallocchio, M. Garlaschè, M. Guinchard, N. Mariani, S. dos Santos, …)

## Slide 2: Outlook
    Context
    HRMT-14 LCMAT experiment
    Irradiation History
    Preliminary Results (Medium Intensity)
    Preliminary Results (High Intensity)
    First Post-irradiation Images
    RF impedance Questions

## Slide 3: Context
LHC beam energy is 2 orders of magnitude above previous machines. Stored energy density is 3 orders of magnitude higher.
Beam-induced accidents represent one of the most dangerous and though less explored events for the LHC.
Novel, yet-to-characterize, composite materials are under development to meet these challenges.
New sophisticated and powerful numerical tools (Hydrocodes) are being used to simulate accidental events.

## Slide 4: Accident Simulations on TCTA
Simulation of direct impact of 8 LHC bunches at 5 TeV on Tungsten Jaw
Probability of water leakage due to very severe plastic deformations on pipes.
Impressive jaw damage:
  Extended eroded and deformed zones.
  Projections of hot and fast solid tungsten bullets (T≈2000K, Vmax ≈ 1 km/s) towards opposite jaw. Slower particles hit tank covers (at velocities just below ballistic limit).
  Risk of “bonding” the two jaws due to the projected resolidified material.
Real Scale Deformations !!

## Slide 5: Novel Materials for Phase II
Primary Collimator
p
e
p
Core
Unavoidable losses
Shower
Beam propagation
Impact parameter
≤ 1 mm
Primary
halo (p)
p
C-C Collimators are affected by intrinsic limitations which may ultimately limit LHC performances:
Low-Z material (Limited Cleaning Efficiency)
Poor electrical conductivity (High RF impedance)
Limited Radiation Hardness (Reduced Lifetime)
Absorber
C-C
C-C
W
W
Super-conducting magnets
SC magnets and particle physics exp.
Courtesy: R. Assmann
Absorber
Phase II Collimator
Secondary Collimator
To overcome this, additional advanced collimators (Phase II) are to complement Phase I
Innovative Materials for Phase II Jaws are the key element for next-generation Collimators

## Slide 6: Novel Materials for Phase II
Metal Matrix Composites (MMC) for advanced thermal management materials combine properties of Diamond or Graphite (high k, low r and low CTE) with those of Metals (strength, g , etc.).
Candidate materials include Copper-diamond (Cu-CD), Molybdenum-diamond (Mo-CD), Silver-diamond (Ag-CD), Molybdenum Graphite (Mo-Gr)

## Slide 7: Material Ranking
Material | C-C | Mo | Glidcop ® | Cu-CD | Mo-CD | Ag-CD | Mo-Gr
Density [g/cm3] | 1.65 | 10.22 | 8.90 | ~5.4 | ~6.9 | ~6.10 | 3.9 ÷ 5.6
Atomic Number (Z) | 6 | 42 | 29 | ~11.4 | ~17.3 | ~13.9 | 10.9 ÷16.5
Tm [°C] | 3650 | 2623 | 1083 | ~1083 | ~2623 | ~840 | ~2520
SSNI [kWm2/kg] | 24 | 2.6 | 2.5 | 13.1 ÷ 15.3 | 6.9 ÷ 10.9 | 11.4 ÷ 15.4 | 7.4 *
TSNI [kJ/kg] | 793 | 55 | 35 | 44 ÷ 51 | 72 ÷ 96 | 60 ÷ 92 | 115 *
Electrical Conductivity [MS/m] | 0.14 | 19.2 | 53.8 | ~12.6 | ~9.9 | ~11.8 | 1 ÷ 18 **
C-C stands out as to thermo-mechanical performances. Adversely outweighed by poor electrical conductivity, low Z, expected degradation under irradiation.
High-Z metals (Cu, Mo) possess very good electrical properties. High density adversely affects their thermal stability and accident robustness.
Metal-diamond composites exhibit a balanced compromise between TSNI, SSNI, electrical conductivity , density, atomic number.
Molybdenum-graphite, currently under development and characterization, shows overall very promising figures of merit.
worse
better
* Estimated values
** with Mo coating

## Slide 8: Why HiRadMat Tests?
To test materials for BID components under the extreme conditions they may encounter in case of accidental beam impacts.
To qualify collimator materials for series production and installation in the LHC, specifically high-Z Tertiary Collimators (TCTA and TCTP).
To quantify collimator damage for LHC Operating Scenarios.
To characterize novel materials currently under development for Phase II Collimators.
To benchmark advanced numerical simulations, extensive but based on limited and scarce literature data on material constitutive models.
To collect, mostly in real time, experimental data on Constitutive Models of BID Materials (Equations Of State, Strength models, Failure Models).

## Slide 9: LCMAT Experiment: Specifications
Type 1 Sample
(Ø 40 mm L30 mm)
Type 2 Sample
(Ø 40 mm, L30 mm,
Surf. Offset 2 mm)
6 different materials (Inermet 180, Glidcop, Molybdenum, Copper-Diamond, Molybdenum-Diamond, Molybdenum-Graphite)
12 Target Stations (Medium intensity and High intensity), with different material samples for each material (Type 1, Type2)
Up to 10 specimens per target station
Extensive Data Acquisition System
Post-irradiation analysis

## Slide 10: Technical Description: Design Overview
Quick Dismounting clamp
Compact experiment Setup
2 axes-movement
Data Acquisition Windows
Specimen holder
Vacuum Tank
Data Acquisition Hardware
Transport structure
Beam

## Slide 11: Technical Description: Design Overview
Fast dismounting system studied to ease tank opening, decreasing exposure time for operators
Vacuum: standard mobile turbo group will allow for pressure below 1mbar
Static structural and buckling analyses performed for tank, glass windows and Be windows. Safety is ok.
Debris generated by beam impacts on samples do not have enough kinetic energy to plastically deform or drill the tank
Stainless Steel vacuum tank: 304L, 10 mm wall thickness

## Slide 12: Technical Description: Vacuum System
Beam line windows in Beryllium, with C/C reinforcements (dimensioning: M. Delonca, C. Maglioni – EN/STI)
Structural and radiation hard, highly transparent optical windows and portholes: fused silica and UHV specific glass adopted
Leak tightness test performed on the assembly
Thermal treatment (vacuum firing) performed on highly outgassing graphite components.

## Slide 13: HRMT-14: Embarked Instrumentation
38 Temperature probes and 1 Vacuum sensor, Microphones (D. Deboy).
244 Resistive Strain Gauges: measuring circumferential and axial strains generated on outer surface (type 1 and 2).
  Amplitude : 1500 up to 20’000 μm/m
  Sampling Frequency: 2 MHz
  Compliant with high radiation levels
Expected circumferential strain on Inermet180, 20 bunches

## Slide 14: HRMT14: Remote Instrumentation
Laser Doppler Vibrometer
Mirror
To Camera
LDV: measuring radial velocity (up to 24 m/s) of outer cylindrical surface (type 1 samples). Sampling rate: 2.5 MHz
High Speed Camera: acquiring live images of impacted type 2 samples. Capture rate 20 kfps. Exposure time 5 ms.
Placed in a bunker 42 m upstream of the experiment.
Restricted Access
No or Very limited Access
Table B

## Slide 15: Energy Deposition
V. Boccone
EN-STI

## Slide 16: Irradiation History
Beam energy: 440 GeV
Bunch spacing: 25 ns
Protons/bunch: ~1.1E11 (lower when scraped)
Beam Pulses: 1 to 24 b/pls on Type 1; 72 or 144 b/pls on Type 2
Beam size: ~1.5x1.5 mm2 (unscraped) on Type 1; ~2x2 mm2 on Type 2
1 to 144 bunches per pulse
Total # bunches: 1558 (excluding alignment)
Total # pulses: 52 (excluding alignment)
Total # protons ~ 1.7E14
Test Runs: 27-28/Sept, 2-4/Oct
Irradiation Summary

## Slide 17: Medium intensity tests on Glidcop
  Glidcop, 72 bunches (scraped), total beam intensity: 4.66e12 p (equivalent to ~42 b)
  σ  1.3x1.3 mm2
  Hoop Strain and Radial velocity on outer surface of Sample 8
  Simulations versus Reality

## Slide 18: High Intensity Tests on Inermet180

## Slide 19: High Intensity Tests on Inermet180
  Simulations versus Reality
Beam
Case | Material | Bunches | p/bunch | Total Intensity | Observed Sample | Velocity
Simulation | Inermet 180 (W,Ni,Cu) | 60 | 1.5e11 | 9.0e12 p | 3rd sample (+Energy) | 316 m/s
Experiment | Inermet (W,Ni,Cu) | 72 | 1.26e11 | 9.05e11 | 2nd sample (-Energy) | ~275 m/s

## Slide 20: High Intensity on Glidcop/1
  Delay Beam – T0 = 22 µs (errors in measurements and in CCC pre-trigger settings).
  Configuration: Simultaneous shot of Flash 3 + 4 at t=3 ms.
   Images acquired between 2.9 and 4 ms after the beam impact!!!!
  Need for higher pre-trigger from CCC!!!
0
4
2
1
5
6
t (ms)
Flash 3
Flash 4
T0 (trigger CCC)
T0 + 1850 µs
1150 µs
Total Lighted time 1.1 ms
Delay Beam – T0
T0 + 2350 µs
650 µs
#58 – 2900 µs
#62 – 3100 µs
#80 – 4000 µs
3

## Slide 21: High Intensity on Glidcop/2
  Delay Beam – T0 = 2022 µs (after asking for 4 ms pre-trigger…)
  Configuration: Simultaneous shot of Flash 3 + 4 at t=2 ms.
   Images acquired between -0.1 ms and 1 ms after the beam impact!!!!
  Successful synchronization between Beam, Video-camera and Flashes!!!
0
4
2
1
5
t (ms)
Flash 3
Flash 4
T0 (trigger CCC)
T0 + 850 µs
1150 µs
Total Lighted time 1.1 ms
Delay Beam – T0
T0 + 1350 µs
650 µs
3
#41 – 2050 µs
#61 – 3050 µs

## Slide 22: Post-irradiation (Type 2 samples)
  72 bunches on Inermet
  72 (center) and 144 bunches (offset) on Molybdenum

## Slide 23
Window covering
Tungsten vapour cloud generated during the beam impact expanded inside the vacuum tank and condensed on the video camera window, covering the window itself preventing further video acquisition.
29 October 2012
Window
Tungsten debris
Picture of the front window after impacts

## Slide 24: Some RF-related questions …
Performance of Molybdenum is significantly better that Inermet180 (Tungsten) and marginally better than Glidcop (Copper) for the same accident scenario (72 SPS bunches)
Molybdenum may be a candidate for Phase II Secondary collimators … what are the consequences on RF-impedance (e.g. as opposed to Copper)?
To further reduce damage exposure, we may envisage to apply a thin Mo coating on a lighter bulk material:
  What is pure Mo minimum required thickness?
  What is the effect of bulk material (e.g. graphite vs. Moly/Graphite)?
What if we do not use any pure Mo coating?

## Slide 25
Greetings from….
“Houston” (CCC)
“Baikonur” (BA7)
Not shown in Houston picture:
Marco Garlaschè

## Slide 26
  Backup slides

## Slide 27: Technical Description: Xenon Flash Lightening System
Modified National/Panasonic PE-145 circuit:
Robust and rad-hard
Excellent luminous output using modified condensers (400V, 3300 µF), lightening time ~ 3.5 ms
Low power requirement (3V to charge condensers)
Flash triggered by high speed relays, measured delay ~650 µs (MSS7 type) and ~1200 µs (SAR90505 type)
System components:
  Xenon lamps on windows sides
  Flash box on tank: condensers and relays board
  Pulse generator & power supply in CCC
Safety issues: potential hazards from condensers
Trigger from CCC
Timing diagram
-3
1
t0
-1
-2
2
3
t (ms)
RelayMSS7 (650 µs)
RelaySAR90505 (1200 µs)
Flash2
Flash1
Flash4
Flash3
Test apparatus examined and approved by safety experts (visit 3/7/12 of C. Bernard and J. Pedersen)

## Slide 28
Flash System:
The use of 2 simultaneous flashes gives rise to a certain overexposure, but permits to see small debris on the dark background between the sample holder and the plate.
The error in the CCC trigger signal has been corrected after the first acquisition permitting a very good synchronization between flashes and beam arrival (~100 µs).
Final Tests & Comparison with Numerical Simulations:
The acquired videos, especially the H6_center on Inermet180, have an acceptable quality and permit to see the particles escaping from the samples.
In addition, the video of the impact on Inermet180 showed a clear agreement with Autodyn SPH simulations, confirming the validity of the proposed models in predicting the damage on the TCT Collimators Jaws.
Final remarks:
The Tungsten hot vapour released during the H6_center impact covered significantly the window, not permitting to acquire further videos at high speed...
Conclusions

## Slide 29: Autodyn: Type 2 Sample
70 bunches 2.5mm
T=17µs
70 bunches 0.25 mm
t=17µs
  PROS sigma 2.5 mm:
  Less vaporized material (window covering)
  Lower density change
  Lower load on Be window
  PROS sigma 0.25 mm:
  Representative of high energetic beam impacts
  (~ LHC Scenario)
  Higher particles speeds

## Slide 30
Remote measurements
Restricted Access
40m
Bunker
For DAQ
No or Very limited Access
  Difficulties for the integration…
  Window
  Vacuum Tank
  Mirror
  Mirror
  Active control of the mirror position ?
40m

## Slide 31: Inermet 72b center s=1.8 mm
  Delay Beam – T0 = 2022 µs
  Configuration: Simultaneous shot of Flash 3 + 4 at t=2 ms.
0
4
2
1
5
t (ms)
Flash 3
Flash 4
T0 (trigger CCC)
T0 + 850 µs
1150 µs
Total Lighted time 1.1 ms
Delay Beam – T0
T0 + 1350 µs
650 µs
3
#41 – 2050 µs
#42 – 2100 µs
#44 – 2200 µs